45$(h1ii45$)	Cubicle system C-BASIC$(kurz9Partition Wall System Type C$)

Made by KEMMLIT-Bauelemente GmbH
Maltschachstr. 37
72144 Dusslingen

Germany
Telephone: (0049) 7072 / 131-0
Telefax: (0049) 07072 / 131-150
info@kemmlit.de - www.kemmlit.de


Construction:

13 mm thick, solid grade laminated (HPL) panels

in a static connection of the profiles and

vandal-resistant hardware.

The quoted construction must be TÜV-approved

(GS seal of approval), approval seal must be provided

together with the quotation.

Options:
Type C-BASIC 2.1: Anodised profiles.

As another option: 
Type C-BASIC 2.2: Powder-coated profiles.

Height:
2000 mm, incl. 150 mm under panel clearance.

As an option:

2135 mm, incl. 150 mm under panel clearance.

Partitions and pilasters (front panels):
13 mm thick, solid grate laminated (HPL) panels

according to DIN EN 438 (16926).

Water-resistant, decay-resistant, resistant to

damage through misuse and very easy to

maintain. All visible edges are bevelled, which

reduces the risk of injury.

Profiles:
Head rail and door stop profiles are to be made as a

three-chamber profile made of aluminium, to ensure

a lasting stability. Absolute accuracy of fit of all

connections by means of CNC-threads and drillings

made in the factory must be ensured. Drillings into the

profiles on site must be avoided. By means of a M12x50

screw connection between head rail (74/43mm) and door

stop profiles (44/45mm) made of stainless steel, an

absolutely warp resistant static connection is provided.

This ensures a lasting, long-living and at any time

re-adjustable connection. Screw connection of the

profiles by means of self-tapping screws is not

allowed for reasons of stability and safety. The

lower edge of the door stop profiles must be

covered with a rounded aluminium plate. Wall

connection by means of U-profiles (30/24mm).

Supporting legs:

# The supporting leg construction consists of a

# stainless steel core (Ø 20 mm ) and a stainless

# steel floor plate. The floor plate allows for a minimum

# 3-times screw connection to the tile joints. Continuous

# height adjustability is ensured by means of a M12 thread

# made of stainless steel within the aluminium joints into

# the vertical door stop profiles. This is safeguarded via a

# counter nut. For reasons of stability plugged connections

# and hollow tubes are to be avoided. To ensure a long-

lasting and permanent floor connection of the cubicles,

all main construction parts used should be solely made

of stainless steel. Solutions with plastic parts are vulnerable

to cleaning agents and shock and therefore barred from

assessment of tender responses.

The durable cover sleeve made of nylon must be able to

be easily lifted to ensure easy cleaning.

As an option: the durable cover sleeve made of aluminium

must be able to be easily lifted to ensure easy cleaning.

As an option: supporting leg construction made entirely of

stainless steel with cover sleeve made of stainless steel.

These must be able to be easily lifted to ensure easy cleaning.

Doors:
made of 13 mm thick solid grade laminate (HPL) panels,

blunt door stop.

All edges are milled, the corners are rounded in a 2 mm

radius.

Integrated rubber profile seal throughout the door stop

profile to ensure noise reduction.

As an option the doors can be provided with finger

protection made of sturdy aluminium tubes situated

between the door hinges on the hinge side.

Furniture / hardware:

3 robust, 3-roller-edge hinges (Ø 20 mm) for each door,

it is therefore not possible to un-hinge the doors. The

hinge connection to the HPL-door must be done

appropriate to the material, connected to the surface of

the door, to avoid a splitting of the panel.

Screw connection to the thickness of the HPL can split

the panel, therefore such solutions are not accepted.

Screw connection to the warp resistant multi-chamber

profiles is done via stainless steel torx screws to provide

easy maintenance.

Rivet connection to the profiles are not adjustable, not

maintenance friendly and are therefore to be avoided.

Each door is to be provided with one hinge with integrated

spring for self-closing or self-opening of the doors.

Hinge axis to be made of stainless steel (Ø 8 mm), spring

made of non-rusting Delta-Seal-Steel to prevent creaking.

The hinge surface is to be made of aluminium for reasons

of material homogeneity of hinges and profiles.

Easily replaceable, free from plastic single latch lock made

of zinc die-cast, with solid non-flammable latch.

Constructions with locking mechanisms that can get jammed

or show signs of wear after heavy usage are not allowed

due to safety reasons.

Lock cover plate made of solid aluminium.

Locking mechanisms made of steel or stainless steel are

undesirable due to material homogeneity. Door knobs made

of crack- and impact resistant nylon.

As an option: door knobs and indicator made of solid

aluminium, satin anodised.

Colours:
Cubicle and door colours according to the KEMMLIT

colour charts (at least 15 colours).

Profiles, hardware, supporting legs and accessories available

in the same continuous colours according to the KEMMLIT colour

chart (at least 8 colours).

All prices ex works in Dusslingen. Taxes and duties

are unpaid, materials only. Installation and transportation

are not included.

/E

45$$NNN

$(h1ii45.10$)		                                                 $(menge0,000$)  no               .$(einhno.$)$(d276$)$(ep.............$)	$(gb.............$)

Accessories for toilet cubicles:

$(langAccessories for toilet cubicles $)
KEMMLIT door stopper hooks made of nylon 301$)

/E

$$NNN

$(h1ii45$$NNN

$(h1ii45.20		                                                 $(menge0,000$)  no               .$(einhno.$)$(d276$)$(ep.............$)	$(gb.............

$(langKEMMLIT wall hooks made of nylon 302$)

/E

45$$NNN

$(h1ii45.30$)		                                                 $(menge0,000$)  no               .$(einhno.$)$(d276$)$(ep.............$)	$(gb.............$)

$(langKEMMLIT paper roll holder made of nylon 308$)

/E

45$$NNN

$(h1ii4.40$)		                                                 $(menge0,000$)  no               .$(einhno.$)$(d276$)$(ep.............$)	$(gb.............$)

$(langKEMMLIT replacement paper roll holder made of nylon 309$)

/E

45$$NNN

$(h1ii45.50$)		                                                 $(menge0,000$)  no               .$(einhno.$)$(d276$)$(ep.............$)	$(gb.............

$)

$(langKEMMLIT WC-brush set, square-shaped, made of nylon 310
45$$NNN

$(h1ii45.60$)		                                                 $(menge0,000$)  no               .$(einhno.$)$(d276$)$(ep.............$)	$(gb.............$)

Accessories are also available in stainless steel.$)

$)

/E$$GRUEnd

----------------------

Cubicle  system$(kurz9Partition Wall system Type C-BASIC$)	$(gb.............$)

============

/E