5$(h1ii$)	$(kurz9Cubicle system NiUU K

$(langMade by KEMMLIT-Bauelemente GmbH
Maltschachstrasse 37
72144 Dusslingen

GermanyGermG
Telephone: 0049 (0)7072 / 131-0
Telefax: 0049 (0)7072 / 131-150
info@kemmlit.de - www.kemmlit.com

Construction:

Construction made of 38 mm thick melamine resin laminated full chipboard panel for row-form installations and lateral cubicles with grooved doors and smooth-surfaced look and feel. On the lock and swing-side with exchangeable door folding, reinforced with metal for protection against vandalism and damage.

Accident prevention as well as product longevity due to TÜV and GS certification.

Height:

2135 mm, including 150 mm ground clearance

Other heights are possible

Walls:

All front wall components are made of 38 mm thick melamine resin laminated full chipboard panel, and interior walls are made of 30 mm chipboard panel. Vertical edges in the area of the door are reinforced with sturdy aluminium edging; all other edges are protected for accident prevention with 3 mm thick ABS edging.

Profiles:

All profiles are made of anodised aluminium and are rounded off to avoid accidents (radius 2 mm).

A rigid stabiliser (45/80 mm) runs over the door front.

As a variant: the rigid stabiliser 40/30 is set back by about 150 mm from the door front.

As a variant: the floor and ceiling attachment profiles are made from sturdy aluminium and present an elegant shadow gap as a crossover to the structure.

The wall attachments are fitted with U profiles in order to balance constructional tolerance.

As a variant: The wall attachments are fitted with shadow gaps to balance constructional tolerance.

Feet:

Elegant, high-quality feet made of corrosion-resistant aluminium (Ø 20 mm), natural colour, anodised with stainless steel core and stainless steel plate.  Height progressively adjustable. Ground clearance of choice, ranging from 80 mm to 215 mm. Force-fitted to the partition wall with a M12 screw joint.  The weight-bearing and age-resistant cover plate made of anodised aluminium is easily lifted for cleaning.

As a variant: elegant, high-quality feet made completely of stainless steel (Ø 20 mm), with stainless steel core and stainless steel plate. Height progressively adjustable. Ground clearance of choice, ranging from 80 mm to 215 mm. Force-fitted to the partition wall with a M12 screw joint. The weight-bearing and age-resistant cover plate made of anodised aluminium is easily lifted for cleaning.

As a variant: optimised ground clearance (50-80 mm) by means of designer foot. To ensure maximum privacy, ease of cleaning and optimal ventilation. Foot made of sturdy aluminium, anodised in a natural colour, force-fitted to the partition wall with a M12 screw joint.

This solution is completely resistant to corrosion, even with aggressive ambient air.

Doors:

Made of 38 mm thick, melamine resin laminated full chipboard. On the lock and swing-side with exchangeable door folding, reinforced with metal for protection against vandalism and damage.

Bands:

2 x 3 roll bands, requiring absolutely no maintenance, non-detachable, specifically lengthened for the object space, made of aluminium, 6 x inserted nuts (Ø 20 mm). One band is fitted with an in-built spring for self-closing or self-opening of the door.

As a variant: 2 roll band made of stainless steel.

As a variant: hidden horizontal special band, integrated flush-mount into the wall and door components. Plugged; not visible from either side for optimal ease of cleaning.

For attachment heights >2135 mm, with an additional 3rd band.

Fittings:

Two-bolt WC lock with L form latch made of anodised aluminium (Ø 23 mm), red/white indicator with wear-resistant metal bolt for emergency opening

As a variant: nylon - U form latch fitting, red/white indicator with emergency opener

As a variant: aluminium - U form latch fitting, red/white indicator with wear-resistant metal bolt for emergency opening

As a variant: Stainless steel - U form latch fitting, red/white indicator with wear-resistant metal bolt for emergency opening

As a variant: Stainless steel - L form latch fitting, red/white indicator with wear-resistant metal bolt for emergency opening

As a variant: Single bolt with rod grip made of sturdy aluminium in 4 variants with LED - indicates red and emergency opening

Colours:

Wall and door colours as per NiUU - KEMMLIT colour chart (at least 18 colours).

Profiles, feet and hinges anodised in aluminium

3 mm ABS edging in white and light grey (Manhattan)

Accessories - exclusive accessories in aluminium or stainless steel

Prices include transport and installation costs.

$)

/E$$GRUEnd

----------------------

$(kurz9Cubicle system NiUU K$)	$(gb.............$)

============

/E