$(h1ii58$)61	$(kurz9Cum Cubicle system classiccell blackedition aluminium $(Addr1Name1$)	$)

Made by KEMMLIT-Bauelemente GmbH
Maltschachstr. 37
72144 Dusslingen
Telephone: (0049) 7072 / 131-0
Telefax: (0049) 7072 / 131-150
info@kemmlit.de - www.kemmlit.de

Construction:

Flush-surfaced aluminium composite elements,

42 mm thick, strike and dent resistant, corrosion-resistant,

with 3-component varnish-coating (Crystal Coat) and

vandal-resistant hardware.

TÜV-approved (GS seal of approval).

Options:
classiccell aluminium 3.1 blackedition: anodised aluminium profiles

classiccell aluminium 3.4 blackedition: stainless steel profiles 

Height:
2000 mm, including. 150 mm under panel clearance.
2135 mm, including. 150 mm under panel clearance.

Other heights are also available.

With 80 mm floor and ceiling clearance, for maximum privacy

combined with highest cleaning friendliness.

Floor-to-ceiling construction with room-height doors

for a maximum privacy also available.

Partition panels and pilasters:

42 mm thick, corrosion-resistant aluminium composite

elements. Environmentally friendly varnish-coating, depending

on colour with a non-sensitive structure (Crystal Coat), scratch- and

UV-resistant according to DIN 53384 A. The aluminium

alloy is seawater-resistant according to DIN 1725.

# The aluminium sheets are canted on all 4 sides.

The inside of the elements is filled with a warp-resistant

inlay. Screw-proof inlays in the composite element

guarantee the long-lasting  and solid fixing of accessories.
 
Profiles: 
The smooth, square shaped aluminium profile (head rail) 54/43

is situated visibly directly above the door front.

# As an alternative square satin anodised aluminium profile 40/30

# As an alternative square stainless steel profile 40/30

# As an alternative concealed head rail integrated in the

# door front.

Wall connections with surrounding U-profiles made of

satin anodised aluminium.

# As an alternative shadow gap wall connection with U-profiles.

Supporting legs:

Anodised aluminium supporting legs (Ø 20 mm), with

stainless steel core and foot plate, adjustable in height.

Force fit connection with the partition by means of a M12

screw connection. The corrosion resistant and durable

aluminium cover sleeve can be easily lifted for cleaning

purposes.

# As an alternative made completely of stainless steel (Ø 20 mm).

# Force fit connection with the partition by means of a M12

# screw connection. The corrosion resistant and durable

# stainless steel cover sleeve can be easily lifted for cleaning

# purposes.

Doors:
Aluminium composite elements, 42 mm thick, with strike and

dent resistant full faced door inlays, corrosion resistant

(same construction as the partition panels and pilasters), rebated.

# Hinges:

2 maintenance-free, impossible to unhinge,

3-roller edge hinges made of satin anodised aluminium,

screwed six times, (Ø 20 mm) with hinge roller extended

to 145 mm. One hinge is equipped with an integrated spring

for either self-closing or self-opening of the doors.

The hinges are tested and guarantee a minimum of 200.000

openings, for this purpose a certificate is to be provided.

As an alternative made of gloss polished aluminium.

As an alternative 2 maintenance-free, impossible to unhinge,

3-roller edge hinges made of brushed stainless steel

(Ø 20 mm), with hinge roller extended to 145 mm.

One hinge is equipped with an integrated spring

for either self-closing or self-opening of the doors.

# Furniture/ hardware:

Double latch lock WC with whisper-comfort-locking function

(low-noise closing), durability ensured by classification according

to DIN EN 12400 minimum category 3 (durability higher than 20.000

operation cycles) as well as DIN 18251-1. Quality lever handle tested

according to EN 1906 class 3 made of satin anodised aluminium.

Locking device made of satin anodised aluminium with

red/white indicator and metal emergency release bolt.

As an alternative made of stainless steel.

As an alternative made of nylon (colours according to the KEMMLIT colour chart).

Single latch lock WC. Door knobs made of satin anodised aluminium.

Locking device made of satin anodised aluminium with

red/white indicator and metal emergency release bolt.

As an alternative made of stainless steel.

As an alternative made of nylon (colours according to the KEMMLIT colour chart).

As an option: single latch lock with grab bar made of solid

aluminium available in 4 versions with LED-indicator and

erosion resistant metal bolt as emergency release mechanism.

Colours:
Panels and door colours in RAL 9005 deep black.

Environmental friendliness:
Only environmentally friendly materials without PVC or CFCs

must be used.

Prices ex works Dusslingen, excluding taxes and duties,

transportation and installation not included.$)

61.10 			$)			$(menge0,000$) $(einhno.$) 	$(d276$)$(ep.............$)	$(gb.............

$(h1ii

$(langAccessories for WC cubicles :

KEMMLIT-door stopper hooks made of  aluminium 4401$)/E

$$NNN

$(h1ii61.20$)			$(menge0,000$) $(einhno.$)	$(d276$)$(ep.............$)	$(gb.............

$)

$(langKEMMLIT-wall hooks made of aluminium 4402$)/E

$$NNN

$(h1ii61.30$)			                             $(menge0,000$) $(einhno.$)	$(d276$)$(ep.............$)	$(gb.............

$)

$(langKEMMLIT-paper roll holders made of aluminium 4408$)/E

$$NNN

$(h1ii61.40$)			                             $(menge0,000$) $(einhno.$)$)	$(d276$)$(ep.............$)	$(gb.............

$)

$(langKEMMLIT-replacement toilet roll holders made of aluminium 4409$)/E

$$NNN

$(h1ii61.50$)			                             $(menge0,000$) $(einhno.$)$)	$(d276$)$(ep.............$)	$(gb.............$)

$(langKEMMLIT-WC brush set made of aluminium 4410
 $)/E$$NNN

$(h1ii61.60$)			                             $(menge0,000$) $(einhno.$)	$(d276$)$(ep.............$)	$(gb.............

Accessories are also available in stainless steel or nylon.

/E$$GRUEnd

----------------------

$(kurz9Cubicle system classiccell aluminium$)	$(gb.............

$)

============/E